## Slide 1
Introduction to Imaging Ellipsometry
Fangqing ZUO
Accurion China, Shanghai

## Slide 2
www.accurion.com
Ellipsometry - Introduction

## Slide 3
( Paul Drude, Lehrbuch der Optik, Leipzig, 1900 )
History……
Karl Ludwig Paul Drude, physicist (1863 - 1906)

## Slide 4
( Paul Drude, Lehrbuch der Optik, Leipzig, 1900 )
( Nanofilm_EP4, Accurion GmbH, Goettingen, 2013)

## Slide 5
incident beam
plane of
incidence
p
p
s
s
E
E
film / substrate system
( Paul Drude, Lehrbuch der Optik, Leipzig, 1900 )

## Slide 6
Ligth source
polarizer
compensator
analyser
detector
sample

## Slide 7
p
s
P
p
A
Nulling ellipsometry
Ligth source
polarizer
compensator
analyser
detector
sample

## Slide 8
NULLING ELLIPSOMETRY
If c = 45°:
 = 2p + /2 (polarizer angle at minimum signal)
 = |a| (analyzer angle at minimum signal)
measurement
Δ , 

## Slide 9
Measure  and 

## Slide 10
Drude equation

## Slide 11
Wavelength or AOI spectra
Optical model
Results
thickness
n, k at different wavelength
volume fraction
(EMA)

## Slide 12
analyser

## Slide 13
analyser
highest accuracy
eliminate system errors
full range without blind zone

## Slide 14
www.accurion.com
Imaging Ellipsometry - Introduction

## Slide 15
Ligth source
polarizer
compensator
analyser
detector
sample

## Slide 16
Ligth source
polarizer
compensator
analyser
CCD
sample
objective

## Slide 17
p
s
P
p
A
Nulling ellipsometry

## Slide 19
FePS3 flake
Regions of interest (ROI)

## Slide 20
Ellipsometric Enhanced Contrast Micrographs
Air|Fe|SiO2(native)|Si
0°
0°
0°
polarizer
compensator
analysator

## Slide 21
Ellipsometric Enhanced Contrast Micrographs
Air|Fe|SiO2(native)|Si
45°
45°
45°
polarizer
compensator
analysator

## Slide 22
Delta-map Psi-map
Microscopic mapping

## Slide 23
Thickness map refractive index map
Microscopic mapping

## Slide 24
Eliminate back-reflection
Air|MoS2|Sapphire

## Slide 25
Eliminate back-reflection
Air|MoS2|Sapphire

## Slide 26
EP4_alignment_sensor:
Accurion has two sub
11

## Slide 27
AFM NaniteB (Nanosurf):
Accurion has two sub
Automatic linear stage
Compact multi-purpose AFM
11

## Slide 28
AFM NaniteB (Nanosurf):
Accurion has two sub
12

## Slide 29
MicroRaman System (Horiba):
Accurion has two sub
Automatic linear stage
Compact Raman probe
14
Multi-axis alignment
Microspot objective

## Slide 30
UV / VIS Reflection Spectrometer RefSpec (Accurion):
Accurion has two sub
Automatic linear stage
17
Multi-axis alignment
Compact sensor head

## Slide 31
QCM-D system E1 (Q-Sense):
Accurion has two sub
20

## Slide 32
Electron synchrotron DESY (Hamburg, Germany):
Accurion has two sub
24
V. Körstgens et al. (2010)
Combining imaging ellipsometry and grazing incidence small angle X-ray scattering for in situ characterization of polymer nanostructures.
Anal Bioanal Chem., 396 , 139-149

## Slide 33
www.accurion.com
Imaging Ellipsometry - Application

## Slide 34
Applications
Light guides for Liquid-Liquid interfaces
L1
L2
Glass pipes inmersed in the upper liquid act as light guide for the beam, avoiding the air-liquid interface and so the undesired displacements of the beam path

## Slide 35
Applications
Light guides for Liquid-Liquid interfaces

## Slide 36
Applications
Light guides for Liquid-Liquid interfaces
Polystyrene at parafin oil-water interface

## Slide 37
Applications
Light guides for Liquid-Liquid interfaces
Cetylpyridiniumbromide at the toluene-water interface

## Slide 38
DMPE
Sphingomyelin
Applications
Air-Liquid interfaces – BAM pictures
Ethyl stearate
Notes: I have organised my talk in the following steps
38

## Slide 39
Applications
Surface plasmon resonance (SPR)

## Slide 40
Applications
SPR - Kretschmann Setup

## Slide 41
Klenkar G, Brian B, Ederth Th, Stengel G, Höök F, Piehler J, Liedberg B (2008) Biointerphases 3: 29-37.
Applications
Surface plasmon resonance (SPR)
Notes: 41

## Slide 42
Applications
Graphene
Notes: 42

## Slide 43
Applications
Graphene
Notes: 43

## Slide 44
Applications
Graphene
Notes: 44

## Slide 45
Applications
Graphene
Notes: 45

## Slide 46
Applications
Graphene

## Slide 47
www.accurion.com
Air|Graphene|SiO2|Si Delta map

## Slide 48
Accurion GmbH
Stresemannstrasse 30 37079 Goettingen, Germany Phone: +49-[0]551.999 60.0 Fax: +49-[0]551.999 60.10 E-Mail: info@accurion.com Web: www.accurion.com
???
For any questions, do not hesitate to contact the Accurion Team!